## Slide 1: Quantifying the wet and dry atmospheric deposition of microplastics in Switzerland
Narain M. Ashta, Empa, Eawag, ETH Zurich
Ralf Kaegi, Eawag
Christoph Hueglin, Empa
TFMM Meeting, Warsaw, 10-12.05.2023

## Slide 2: What are microplastics?
Plastic particles < 5 mm and > 1 µm in diameter
  > intentionally produced for industrial and commercial uses (e.g. cosmetics)
  > unintentionally generated from larger plastic items or synthetic textiles
Morphology: fibers, fragments, films, foams, spheres/beads
Detected in air, soil, water, snow, sea ice, biota, food, blood etc.
Properties: extreme persistence, potential for long-range environmental transport
Environmental hazards and adverse health effects: largely unknown
Cai et al. 2017
Notes: plastic-free setup to minimize contamination
sampling duration  1 year
sampling frequency  weekly to monthly (depending on meteorological conditions)

## Slide 3: Atmospheric microplastics research
Microplastics (MP) in air reported in 2015 (Dris et al., 2015)
Atmospheric transport to remote regions reported in 2019 (Allen et al., 2019)
Since then, many studies reporting MP in air/deposition samples
Notes: plastic-free setup to minimize contamination
sampling duration  1 year
sampling frequency  weekly to monthly (depending on meteorological conditions)

## Slide 4: Atmospheric microplastics research
Research gaps:
Lack of harmonized sample preparation and analytical methods for MP
  > difficult to compare results across studies
Lack of data on particle recovery rates throughout analytical chain
  > particle losses during sample treatment not tracked
  > significant uncertainties in currently reported MP concentrations
Notes: plastic-free setup to minimize contamination
sampling duration  1 year
sampling frequency  weekly to monthly (depending on meteorological conditions)

## Slide 5: FOEN-funded parallel projects on microplastics analytics
Narain M. Ashta
Guillaume Crosset-Perrotin
Angélique Moraz
Thomas Bucheli
Ralf Kägi
Christoph Hüglin
5
Julie Tolu
Michael Sander
atmospheric deposition
soil
sewage sludge
surface waters (rivers)
Kristopher McNeill
Research projects funded by the
Swiss Federal Office for the Environment
(FOEN)
3/2022 – 2/2026
Add-on project on atmospheric
deposition of tire wear
(funded by the Swiss Federal Roads Office FEDRO) 8/2023 – 7/2025
Icons created by Freepik - Flaticon
Expertise and advise from

## Slide 6: Goals of atmospheric MP project
Develop harmonized method for measuring MPs across different environ-mental compartments (atmosphere, sewage sludge, water and soil)
Monitor wet & dry atmos. deposition of MP across Switzerland
Determine the types and amount of MP entering the environment via the atmosphere in Switzerland (with add-on project incl. tire rubber)
Notes: plastic-free setup to minimize contamination
sampling duration  1 year
sampling frequency  weekly to monthly (depending on meteorological conditions)

## Slide 7: Monitoring of wet and dry deposition rates
Selected NABEL sites
for MP monitoring
Urban
Suburban
Rural
Remote
1 year monitoring (07/2023 – 06/2024)
One-month sampling interval

## Slide 8: Wet & dry sampler for collecting deposition
dry deposition
collected in glass bowl
wet deposition
collected in glass bottle
recovery of surrogate standards
71-77%
recovery of surrogate standards
18-57%

## Slide 9: Modified sampler for collecting wet deposition
wet deposition
collected in glass bottle
collect size-separated particles
Directly during sampling
test version of
cascade filtration unit
(metal version is currently manufactured)
200 µm
5 mm
20 µm
<20 µm

## Slide 10: How are MP measured?
Vibrational spectroscopy: Fourier transform infrared (FTIR) (detection limit ~20 µm), Raman (1 µm)
(particle-based, non-destructive technique)
intensity (a.u.)
wavenumber (cm󠄂−1)
Figure by Bruker Corp.
FTIR spectra of polyethylene (PE)
Thermogravimetric methods: Pyrolysis-Gas Chromatography-Mass Spectrometry (Py-GC-MS), TED-GC-MS
(bulk-method)
Sample pyrolyzed at high temperature (in absence of oxygen)
Degradation products of different chemicals in sample are formed, separated and measured
Unique markers for different polymers are used to identify and quantify mass of polymers in sample
Py-GC-MS
Notes: Sample irradiated with IR light, response of particles at different wavenumbers are Fourier transformed to spectra, spectra matched with reference database
Sample pyrolyzed (heated in absence of oxygen), degradation products separated and their spectra analysed, spectra of unique markers used to determine mass of polymer

## Slide 11: Sample treatment and analytical chain
take optical image of filter
> identify polymer types
> calculate recovery rate
of reference MPs
deposit particles onto filter
separate by size, density and
composition
> particle shape, size, color
extract particles
of interest
FPA-µ-FTIR
chemical analysis
Py-GC-MS
cross-validate results
mass- vs. count-based
count and add
reference MPs
to collection vessels
collect
samples
filtration
200 µm
5 mm
20 µm
<20 µm
currently
Notes: filtration

## Slide 12: Atmospheric dry deposition sample
reference MP
tire wear particle
pollen
natural or synthetic fiber?
plant fiber
dust
dry deposition on aluminium oxide filter (without sample treatment)
2 mm

## Slide 13: Atmospheric wet deposition sample
ve
without sample treatment
oxidative treatment

## Slide 14: Atmospheric wet deposition sample
oxidative treatment

## Slide 15: Chemical analysis using FPA-FTIR
infrared beam
filter
transmission
mirror
wavenumber (cm󠄂−1)
Intensity (a.u.)
1 FPA scan:
area = ~0.12 mm2
time = ~45 seconds
no. of spectra = 4096
match with database
polyethylene (PE)
~ 3 days to analyze entire ⌀25-mm filter (1 sample)
Non-destructive technique
⌀25-mm filter
area = ~490 mm2
no. of FPA squares = ~4088
total no. of spectra = 16.8 million
for routine analysis
sub-sampling (~ 20%)

## Slide 16: Example MP particle found in wet deposition

## Slide 17: Deposition rate based on FPA-µ-FTIR
Deposition rate =
number of MPs identified
fraction of filter analysed × sampling area × sampling duration
(MPs / m2 / day)
Mass flux =
Σ (volume of particle × density of corresponding polymer)
fraction of filter analysed × sampling area × sampling duration
(g / m2 / day)

## Slide 18: Dry deposition rate of MPs in Dübendorf
~50% of filter analyzed using FPA-µ-FTIR
20 MPs detected
  > polymer types: PP, PE, PET, PMMA, PA, PAN/ABS
  > fragments and fibers
dry deposition
22 June – 26 July, 2022
however...
uncertainties with FPA-µ-FTIR measurements
Deposition rate ~ 30 MPs / m2 / day
suburban

## Slide 19: Uncertainties with FPA-µ-FTIR measurements…
Undetected reference particles
Detected reference particles

## Slide 20: Summary
There is a lack of harmonized analytical methods for environmental microplastics
Results of available studies are therefore difficult to compare. Uncertainties of available studies are mostly unknown
For nanoplastics (< 1 mm) the situation is even worse
MP is transported through the atmosphere and deposited into the environment. The types and the amounts of MP depositing from the atmosphere are largely unknown
Effects of MP in the environment are also not well understood today
Research on environmental MP is needed

## Slide 21: Thank you for your attention
Questions?
Many thanks to
FOEN for supporting all three MP projects
Colleagues from Agroscope, Eawag and ETH Zurich
Notes: dry deposition

## Slide 22: …due to slight bending of filter
aluminium oxide filter
Calibration done at one point
slightly bent
Measurements made over large areas
out of focus
microscope stage

## Slide 23: Resolving the filter bending issue
filter holder to flatten filter (in development)
Figure by Guillaume Crosset-Perrotin
and/or use of calcium fluoride windows
(IR transparent material) to press filter
calcium fluoride window
calcium fluoride window
aluminium oxide filter

## Slide 24: Challenges with sub-sampling
Primpke et al. 2017
dry deposition, Dübendorf, 26 Jul – 17 Aug, 2022
“Ring effect”
uneven distribution
of particles on filter
resolve by using
pressure filtration
instead of
vacuum filtration
(to be confirmed)